**Common Nail**

**Description:**

|  |  |
| --- | --- |
| Common nails | |
| Material | Low carbon steel wire Q195, Q235 |
| Length | 3/8’’ --7’’ |
| Shank diameter | BWG4--BWG20 |
| Surface | Polish/bright, galvanized |
| Head | Flat head, round head, checkered head |
| Usage | Building construction, decoration field, bicycle parts, wooden furniture, electrical component, household and so on |
| MOQ | One ton for each size |
| Packing | a . 1kg/plastic bag , 20-25kg/carton  b. 5kg/box, 8boxes/carton  c. 20-25kg/carton in bulk |

**Specification:**

|  |  |  |
| --- | --- | --- |
| **Length** | | **Diameter** |
| *inch* | *mm* | *BWG* |
| 1/2’’ | 12.7 | 20/19/18 |
| 3/4’’ | 19 | 19/18/17 |
| 1’’ | 25.4 | 17/16/15/14 |
| 1-1/4’’ | 31.7 | 16/15/14 |
| 1-1/2’’ | 38 | 15/14/16 |
| 1-3/4’’ | 44.4 | 14/13 |
| 2’’ | 50.8 | 14/13/12/11/10 |
| 2-1/2’’ | 63.5 | 13/12/11/10 |
| 3’’ | 76.2 | 12/11/10/9/8 |
| 3-1/2’’ | 88.9 | 11/10/9/8 |
| 4’’ | 101.6 | 9/8 |
| 4-1/2’’ | 114.3 | 8/7 |
| 5’’ | 127 | 7/6 |
| 6’’ | 152.4 | 6/5 |
| 7’’ | 177.8 | 5/4 |