**Roofing Nail**

**Specification:**

|  |  |
| --- | --- |
| Umbrella Head Roofing Nails | |
| Material | Q195, Q235 |
| Shank Diameter | BWG 9 to BWG 13 |
| Length | 1-3/4" to 3" |
| Head diameter | 14mm-20mm |
| Surface | Electro-galvanized |
| Shank | Twisted, Smooth |
| Head | Umbrella head |
| Color | Shining, blue-white, iron, red etc. |
| Packing | a.  In wooden carton, 7Ibs/box, 8boxes/carton, or 6boxes/carton,  b.  In wooden carton, In 20kg, 30kg, 35kg, 48kg  c.  20kg or 25kg/carton  d.  In Gunny Bags, 25 or 50kg/bag |

**Normal size:**

|  |  |  |  |
| --- | --- | --- | --- |
| Roofing Nails Specification | | | |
| Size | Length (mm) | Shank Diameter(mm) | Head diameter(mm) |
| BWG8\*2" | 50.8 | 4.19 | 20 |
| BWG8\*2-1/2" | 63.5 | 4.19 | 20 |
| BWG8\*3" | 76.2 | 4.19 | 20 |
| BWG9\*1-1/2" | 38 | 3.73 | 20 |
| BWG9\*2" | 50.8 | 3.73 | 20 |
| BWG9\*2-1/2" | 63.5 | 3.73 | 20 |
| BWG9\*3" | 76.2 | 3.73 | 20 |
| BWG10\*1-3/4" | 44.5 | 3.37 | 20 |
| BWG10\*2" | 50.8 | 3.37 | 20 |
| BWG10\*2-1/2" | 63.5 | 3.37 | 20 |
| BWG11\*1-1/2" | 38 | 3.02 | 18 |
| BWG11\*1-3/4" | 44.5 | 3.02 | 18 |
| BWG11\*2" | 50.8 | 3.02 | 18 |
| BWG11\*2-1/2" | 63.5 | 3.02 | 18 |