**Galvanized Steel Coil**

**Specification:**

|  |  |
| --- | --- |
| Product name | Galvanized steel coil |
| Material | Q195, Q235, SGCC, DX51D |
| Standard | GB, ASTM, AISI, DIN |
| Width | 600mm--1250mm(+/-0.02mm) |
| Thickness | 0.20mm--1.2mm (+/-0.15mm) |
| Zinc coating | 40g--275g |
| Technique | Hot-dipped galvanized |
| Spangle | Zero/regular/big/minimized spangle |
| Surface treatment | Chromated, non oiled, skin passed |
| Coil weight | 3--8 MT or as required |
| Packing | Each coil packed with galvanized steel strip |

**Packing:**

Mill's standard export packing.

The coil should be wrapped with waterproof paper.

The after fully wrapped with high density PE film.

The after fully covered with iron sheet with metal edge protectors, strapped with metal bands,

min 4 bands horizontal, min 4 bands vertical.

**Applications:**

1. Construction: roof and roof component, outside walls of civilian and industrial buildings, garage

doors and window blinds.

2. Household appliances: washing machine, refrigerator, television, air conditioner and ventilation

system, Vacuum cleaner, solar water heater.

3. Transportation: car ceiling, auto Industry Muffler, heat shields of exhaust pipe and catalytic converter,

the ship bulkhead, highway fence.

4. Industry: industrial Instruments Electric control cabinet, industrial refrigeration equipment, automatic

vending machine.

5. Furniture: lampshade, counter, signboard and medical facility etc.