**Black Annealed Wire**

**Soft Black Annealed Wire**known as black oil iron wire or black annealed wire.

The soft annealed wire is more economic than the Cold drawing hard wire for making nails.

Black annealed wire is mainly processed into coil wire, spool wire or big package wire.

Or further straightened and cut into cut wire and U type wire.

Black iron wire is mostly used in construction or used as tie wire or baling wire in building,

 parks and daily binding.

**Annealed wire** is though wire-drawing and anneals to finish.

**Black oiled wire** is formed via the processes: wire-drawing, anneal, and fuel oil injection.

**Details:**

**♦ Material:** SAE 1006, Q195

**♦ Diameter:** 0.5mm- 4.5mm

**♦ Tensile Strength:** 30-70kg/mm2

**♦ Elongation:** 10%-25%

**♦ Weight:** 1kg-800kg/coil

**♦ Packaging Details:**

1. Inside with plastic film and outside with hessian

2.Inside with plastic film and outside with woven bag

3**.** In wooden case and as your inquiry.