**Galvanized Wire**

**Galvanized wire is used in weaving of wire mesh, fencing for expressway and construction.**

|  |  |
| --- | --- |
| **Item** | high quality galvanized iron wire |
| **Steel Grade** | Q195 |
| **Coil Weight** | 1kg-800kgs/coil as request |
| **Diameter** | 0.5mm-5.0mm |
| **Zinc Coating** | 10-280g/m2 |
| **Tensile Strenght** | 350-550N/mm2 |
| **Application** | Binding wire, weaving of wire mesh |
| **Packing** | Plastic film inside and outside woven bag  Plastic film inside and outside hessian cloth |

|  |  |  |
| --- | --- | --- |
| **Brif Introduction for galvanized iron wire** | |  |
| **Galvanized iron**  **wire raw material** | Q195 wire rod-this type of wire rod has less impurities so it very suit for drawing. |  |
| Q195 material's chemical component is nearly same as SAE 1006. |  |
| Q195 material chemical component : C≤0.07; S≤0.023; Si≤0.09; Mn≤0.32; P≤0.025. |  |
| **Galvanized iron**  **wire zinc coating** | Electro galvanized: zinc 10-30G/M2; |  |
| Tensile:300-550N/MM2 |  |
| **Galvanized iron wire production process** | Steel rod coil---wire drawing---wire annealing---rust removing---aciding washing---boiling---drying---zinc feeding---wire coiling |  |
|  |

We also supply galvanized straight cut wire.

**Straight Cut Wire**,is a kind of Galvanized steel wire which is cutting to certain sizes after being straightened. **Galvanized Wire**

**Galvanized wire is used in weaving of wire mesh, fencing for expressway and construction.**

|  |  |
| --- | --- |
| **Item** | high quality galvanized iron wire |
| **Steel Grade** | Q195 |
| **Coil Weight** | 1kg-800kgs/coil as request |
| **Diameter** | 0.5mm-5.0mm |
| **Zinc Coating** | 10-280g/m2 |
| **Tensile Strenght** | 350-550N/mm2 |
| **Application** | Binding wire, weaving of wire mesh |
| **Packing** | Plastic film inside and outside woven bag  Plastic film inside and outside hessian cloth |

|  |  |  |
| --- | --- | --- |
| **Brif Introduction for galvanized iron wire** | |  |
| **Galvanized iron**  **wire raw material** | Q195 wire rod-this type of wire rod has less impurities so it very suit for drawing. |  |
| Q195 material's chemical component is nearly same as SAE 1006. |  |
| Q195 material chemical component : C≤0.07; S≤0.023; Si≤0.09; Mn≤0.32; P≤0.025. |  |
| **Galvanized iron**  **wire zinc coating** | Electro galvanized: zinc 10-30G/M2; |  |
| Tensile:300-550N/MM2 |  |
| **Galvanized iron wire production process** | Steel rod coil---wire drawing---wire annealing---rust removing---aciding washing---boiling---drying---zinc feeding---wire coiling |  |
|  |

We also supply galvanized straight cut wire.

**Straight Cut Wire**,is a kind of Galvanized steel wire which is cutting to certain sizes after being straightened.